## Slide 1
PLASTIC RESINS AND FIBERGLASS OPERATIONS
NACT Course 261
Notes: CLASSROOM SETUP:
Check classroom layout
Instructor name/date/course title on board or easel
CDs, name cards, markers, agenda, handouts on desks
Handouts – “WHAT IS CULTURED MARBLE?”; AP-42 Emission Factors; Unified Emission Factors for Open Molding of Composites; Emission Factors for Polymer Casting; SJVUAPCD P/O.
Setup equipment and verify operation
Setup display materials
Locate bathrooms and emergency exits/procedures
INTRODUCTORY REMARKS:
Fill out name tents, tracking cards, sign-in sheet. "Please write legibly as you want your name to appear on your certificate. Include company name and address."
Agenda highlights - lecture, breaks, lunch, exam, field inspection trip, safety gear requirements, certificate. Have students turn off cell phones and set beepers to stun.
Introduce yourself, background, and experience.
Student background, experience, expectations.
Aims of 200-Series training program: [ THE CALIFORNIA VERSION ]
• Inspector-oriented
PROVIDE OPERATIONAL AND THEORY BACKGROUND
• Details of process/systems and practical inspection techniques
• Facilitate communication and share experiences
Topics to be covered - refer to agenda, handouts, or overview slide
Student Course Manual - review contents, indicate how used
Handouts - indicate how will you be using them. Discuss show and tell materials.
Additional information - instructor discretion

## Slide 2
OZONE Formation
Notes: Ozone formation patterns from 8:00 am to 11:00 pm.

## Slide 3
Plastic resin uses
Plastic resin theory / operation
Air pollution control devices
Implementing regulations
Typical permit conditions
Inspection procedures
Federal regulations
Course Overview
Notes: Cover course overview.
Stated as objectives, upon completion of this course, you should:
Be familiar with some industrial uses of plastic resins.
Using appropriate terminology, be able to explain the theory of operations of polyester and epoxy resins.
Be able to describe the major methods and devices used in controlling air contaminant emissions from polyester resin operations.
Be familiar with some of the implementing HAP emission control regulations.
Be familiar with some typical polyester resin permit conditions.
Be able to explain how to conduct an inspection of a polyester resin operation.

## Slide 4: Uses of Polyester Resins
Aircraft / Aerospace / Automotive
Marine / Railroad applications
Electrical / Electronic components
Construction / Building materials
Packaging materials
Consumer / Institutional products
Corrosion resistant products
Business equipment
Furniture / Furnishings

## Slide 5
Composite Decking
Notes: ChoiceDek : Low-maintenance decking product
Manufactured from a blend of recycled :
Polyethylene plastics (50%)
Recycled wood fibers (50%).
Wood fibers are co-mingled in plastic.
The plastic surrounds and bonds to the wood fibers
 Making them virtually moisture proof.
Wood fibers reinforce the plastic
 Making it stiffer
 Reducing its thermal movement.

## Slide 6
Structural strength & rigidity
Heat resistance
Corrosion resistance
Dielectric strength
Design flexibility
Low finish cost
Moisture resistance
Reuse & recycle
Light weight
Durable
Advantages
Notes: Dielectric Strength : Measure of electrical insulation

## Slide 7: Disadvantages
VOC emissions
Toxicity issues
Flammability
Storage
Disposal

## Slide 8: Emissions From Polyester Resins
Ethylene
Styrene / MMA
Ethylene Glycol
Pentane
Acetone / MEK
MEKP
Dibasic Ester
Resins
&
Glass
Fiber
Notes: Styrene and MMA (Methyl Methacrylate) are HAPs
MEKP is a catalyst • initiator • accelerator
→ controls the rate of reaction
→ highly toxic (severe skin irritant)
→ highly unstable
→ highly explosive
TQ
15

## Slide 9
Plastic
  Organic compounds that can be molded
Polymer
  Two or more like molecules joined to form a more complex, physically different molecule
Resin
  Carbon compound polymers used in reinforced products to surround and hold fibers
Common Terms
Notes: Plastics generally are : Organic, high molecular weight polymers
 consist of large chains of CARBON molecules

## Slide 10
Consist of building blocks : HC
  Derived from petroleum or NG
  Monomers (mono=one, mer =unit)
  Bonded into chains  Polymers
Reaction known as Polymerization
  Ethylene  Polyethylene
  Propylene  Polypropylene
How are Plastics made?
Notes: Monomer : low molecular weight organic compound. Aka: “mer”
(e.g. : Styrene)
POLYMERIZATION (aka: CURING)
Combines (bonds) with other compounds :
 by cross-linking reaction
 to become cured, thermosetting resin

## Slide 11
Let’s Discuss Common Plastics

## Slide 12
Polycarbonate
Polyethylene
Polystyrene
Polypropylene
Polyurethane
Polyvinyl Chloride
Polyesters
Common Plastic Materials
Notes: Polycarbonate
Polyethylene
Polystyrene “We’ll cover each
Polypropylene focusing primarily on
Polyurethane polyesters and polystyrene”
Polyvinyl Chloride
Polyesters
University of Southern Mississippi
School of Polymers & High Performance Materials
Polymer Science Learning Center @
http://www.pslc.ws/macrog/kidsmac/polysty.htm

## Slide 13
Created to compete with die-cast metals
Strong, tough & rigid
Excellent electrical insulators
Mostly electrical uses
Polycarbonates

## Slide 14
Clear, very tough polymer
Excellent barrier against O2 and CO2
Good chemical resistance
Soft drink bottles
Fiber (the polyester 70s!!!)
Magnetic tape (audio & video)
Polyethylene : PET
Notes: Soft drink, water, beer, juice, food and
custom container applications

## Slide 15
Polyester Fiber Jacket
Notes: Materials are 100% polyester and used exclusively in outerwear and sleeping bags

## Slide 16
Fleece Made From
Recycled “PET”
Notes: Made of Polyester fibers
About 50% comes from recycled bottles

## Slide 17
PET
Product

## Slide 18: High Density Polyethylene
High density version of PE
Excellent protective barrier properties & Strong
Milk, juice & H2O container
Household chemicals
Detergents
Notes: Strong plastic material

## Slide 19
High Density
Polyethylene

## Slide 20: Low Density Polyethylene
Low density version of PE
Offers clarity & flexibility
Provides ductility
Grocery & garbage bags
Shrink & stretch films
Notes: Very ductile material

## Slide 21
Composite Decking
Notes: Made from recycled Polyethylene composite deck

## Slide 22: Polypropylene
“Workhorse” of plastics
High tensile strength
High melting point
Good chemical resistance
Packaging & carpeting
Automotive & appliances

## Slide 23
Foamed or Expanded Polystyrene : EPS
Exceptional insulation properties
Foam cups & containers
Foodservice products
Packaging & protecting
Polystyrene
Notes: • CD Cases
• Plastic Spoons & Forks
(Perhaps) Biggest use of EPS is now in Major Building Construction (Walls and Floors)
EPS: → 95% air
→ 5% polystyrene
→ made by a blowing agent (Pentane or CO2)
→ STYROFOAM® = Dupont trademark

## Slide 24
Expanded Polystyrene
Foam

## Slide 25
Recycled Polystyrene

## Slide 26
Recycled Polystyrene
Baseboard Molding

## Slide 27
Foam : bedding, auto seats, cushioning, carpet underlay
Insulation & flotation
Polyurethane coatings
Abrasion resistant : printing rolls, conveyor belts, gaskets & seals
Polyurethanes
Notes: What is flexible polyurethane foam (FPF) ?
FPF is a chemically complex polymeric product having a broad range of load bearing capability and resiliency, offering comfort as cushioning material for furniture, bedding, carpet underlay, and automotive interiors. FPF also offers protective shock absorption performance for use in packaging and automotive applications.
In furniture and bedding applications, short staple polyester fiber is often used instead of FPF, as is cotton, but both alternative materials have poor height recovery characteristics after compression. Comparing FPF to alternative materials in the areas of economics, comfort potential, ease of use, and durability, there is not an acceptable substitute for FPF.

## Slide 28
Polyurethane
Foam

## Slide 29: Polyvinyl Chloride (PVC)
Chemical, abrasion & weather resistance
Pipes & sidings
Leather-like upholstery
Gloves, boots & apparel

## Slide 30
What are Composites?

## Slide 31: Introduction to Composites
Made up of 2 or more components
  Fibrous reinforcing network embedded in the cured resin matrix
  Types of reinforcements
   Fiberglass, Carbon fiber & Kevlar
  Thermosetting type resin is a plastic that cures from a liquid to a solid state
   Polyester, Vinyl, Epoxy & Urethane
Notes: Combination of 2 or more materials
1. Binder Material (Resin)  Matrix
2. Other Material  Reinforcement
Properties & Structural performance of the composite are superior…
… to those of the constituents acting independently.
“The three primary types of reinforcements used to make composites are fiberglass, carbon fiber and Kevlar.”
TQ
11

## Slide 32
Composite
Material

## Slide 33
Types of
Reinforcements
• Fiberglass
• Carbon Fiber
• Kevlar

## Slide 34: Carbon Fiber
Stiffest & strongest reinforcing fibers for polymer composites
Used together with epoxy
Race cars
Space applications
Sporting equipment
Notes: Carbon fibers mostly improve the strength to weight ratio.

## Slide 35
Carbon Fiber

## Slide 36
Carbon Fiber

## Slide 37
Carbon Fiber Product

## Slide 38
Made of silicon oxide
Produced by a spinning process
Pulled through a nozzle from molten glass
Reinforcing materials
Automotive and naval industries, sporting equipment
Fiberglass
Notes: Raw Materials : More than half the mix is silica sand, the basic building block of any glass. Other ingredients are borates and trace amounts of specialty chemicals.
Batch House : The materials are blended together in bulk quantity, called the "batch." The blended mix is then fed into the furnace or "tank."
Fiberglass is produced by a spinning process during which molten glass is pulled through a nozzle.
(thousands of meter/min).
TQ
10

## Slide 39
Fiberglass Forms

## Slide 40: Fiberglass Forms
Surfacing Mat (Veil)
Chopped Strand Mat
Roving (Spool)
Woven Roving
Cloth (Hand Lay-up)
Notes: Surfacing Mat : Thin layer of fine, soft fiberglass used next to Gel Coat. Used for Special Jobs (complex shapes).
Highly Resin Rich zone
Chopped Strand Mat : Mat form of fiberglass reinforcement. Multi-directional strength. Made of chopped strands (2” long) held together by a binder (soluble in resin). Mat is used to inexpensively build up bulk and increase strength and stiffness.
Roving : Wound in a cylindrical package (least costly). Loose twine of fiberglass / Chopped & fed with resin onto Mold.

## Slide 41
Fiberglass
Forms

## Slide 42
Fiberglass
Forms

## Slide 43
High strength
Low price
Dimensional stability
Temperature resistance
Corrosion resistance
Low weight
Excellent dielectric properties
Fiberglass Advantages

## Slide 44
Fiberglass Product
Notes: This motorboat hull is made of glass reinforced polyester by hand lay-up.
This allows to produce a light boat with a very smooth surface.

## Slide 45
Fiberglass
Spa

## Slide 46: Types of Fiberglass
E-glass and S-glass
  E-glass  Good electrical properties
  S-glass  Very strong, stiff, and temperature resistant
Notes: There are two main types of glass fibers:
E-glass and S-glass.
E-glass is the most used, and takes its name from its good electrical properties.
S-glass is very strong, stiff, and temperature resistant.

## Slide 47: Glass Fiber Reinforced Resin
Most used composites
Temp resistance & strength
Impregnating fibers with liquid epoxy resins
Aircraft components
Casings for missiles, pipes, tanks, pressure vessels
Notes: Glass reinforced resins are the most used composites.
 Low price…... combined with……..
 Good mechanical strength.

## Slide 48: Kevlar
Lightweight Flexible Comfortable
High Tensile Strength
Excellent Dimensional Stability
High Flame Resistant
High Chemical Resistant
Used with epoxy or vinyl resin
Notes: Advanced tech. from  DUPONT
Manmade Synthetic Fiber
5 times stronger than steel
(on a equal weight basis)

## Slide 49
Kevlar Product
Notes: B-2 Stealth Bomber
Made by : Hand Lay-up
Kevlar Composite : Cross Layers
Continuous Curvature  Reflects Radar
Easy to control fibers orientation.
Process is very flexible
different kinds of geometry

## Slide 50
Protective & Performance Apparel
Composites : aircraft parts/boats
Fiber-Optic Cables
Tires
Ropes & Cables
Brake Pads & Clutch Linings
Power Transmission Belts / Hoses
Kevlar

## Slide 51
Kevlar
Product
Notes: Blackhawk Helicopter
Body is mostly composite material

## Slide 52
Let’s Discuss Types of Plastic Materials

## Slide 53: Types of Plastic Materials
Thermoplastic Resins
  Become fluid upon heating
  Repeatable & reversible process
  No chemical change
  No permanent change in physical prop.
  Readily extruded or molded
  E.g.. film, fibers, bottles etc.
  Polyethylene, Polystyrene & Polypropylene
Notes: All polymers fall within one of 2 basic groups: thermosetting & thermoplastics.
A thermoplastic resin has a linear molecular structure that will repeatedly soften when heated to its melt temperature and harden when cooled.
In simple terms, a thermoplastic is comparable to paraffin wax, which flows when heated and hardens to a set shape when cooled. [ REVERSIBLE STATE ]
Examples : polypropylene, polyethylene, polystyrene, nylon, polycarbonate.
TQ
23

## Slide 54: Types of Plastic Materials
Thermosetting Resins
  Irreversibly polymerizes and solidifies
  Chemical structure permanently altered
  Cannot be resoftened
  Process called curing or hardening
  E.g.. Molding, casting, powder coating
  Polyurethanes, Polyester & Epoxy resins
Notes: A thermosetting, or thermoset, resin "cures" into an irreversible state because its molecular structure is cross-linked.
A thermoset resin is comparable to an egg. Once it's cooked, it essentially stays in the same state.
Examples : unsaturated polyester, vinyl ester, epoxy and urethane.

## Slide 55: Thermoplastic vs. Thermosetting
Thermoplastic Thermosetting
Faster molding Design constraints
Lower emissions Limited unit production
Lower costs Performance requirements Easy recycling Market demands
Low labor intensity

## Slide 56
Resins Fiberglass
Fiber substrate Catalysts
Additives Solvents
Initiators
Raw Materials
Notes: Methyl Ethyl Ketone Peroxide - Most common Room Temp. Catalyst
Function is to crosslink the resin - causing it to gel and then cure.
Reactive agent that brings about polymerization when it is added to a resin
Gel Coat - A quick setting polyester resin coating applied to the mold surface. Function is to protect the fiberglass from the environment. Used to improve surface appearance and bonding.

## Slide 57
Typical Raw Materials

## Slide 58
What is a Resin?
Notes: RESIN - A material, generally a polymer, that has an indefinite and often high molecular weight and a softening or melting range and exhibits a tendency to flow when it is subjected to stress.
Resins are used as the matrices to bind together the reinforcement material in composites.
RESIN CONTENT - The amount of resin in a laminate expressed as either a percentage of total weight or total volume.

## Slide 59: Thermoset Resins
Two Common Types
 Epoxy & Polyester
 Molding, Laminating, Casting ….
  Epoxy
   Higher Performance & Higher Price
   High Strength, Weight Critical
   Dimensionally Accurate Applications
Notes: EPOXY : 2 and 1/2 times the cost of Polyesters.  Relatively expensive
Epoxy has :
 Best mechanical properties
 Good thermal resistance
 Difficult to process
Its shrinkage factor is less that Polyester.
Thus close tolerance laminates, such as precise tooling, are made with epoxy.

## Slide 60
Epoxy
Resin
Product
Notes: Where highest strength-to-weight ratios are required, as in aircraft parts, epoxies are used.
Thunderbirds : US Air Force

## Slide 61: Polyester Resins
Building Blocks for Polyester Resins
Acids & Glycols Cooked Together
Dissolved in Styrene Monomer
Inhibitors Added to Delay Reaction
Product Added to a Peroxide Catalyst
    Unsaturated Portions of Monomer and Polyester React Together
Hard Solid Mass
Notes: Polyesters are macromolecules prepared from different dibasic acids (such as isophthalic, orthophthalic, terephthalic acids, fumaric/maleic acids) and diols (dihydric alcohol) such as ethylene glycol, propylene glycol, neopentyl glycol, bisphenol A (BPA) etc.
Polyester resins are generally classified as ortho resins, iso-resins, BPA fumarates, vinyl ester resins.
Different combination of these di-acids & diols due to difference in their structures impart variation in mechanical properties like flexural strength, tensile strength, and compressive strength.

## Slide 62
Polyester Resins

## Slide 63: Fabrication With Polyesters
Reinforcements such as a Glass Fiber in a Mold
Saturated with Polyester Resin
Resin Mixed with Catalyst Causing Crosslinking Reaction
This Causes Resin to Harden from Liquid to Solid
Polyester Resin in Fiberglass Boat Mfg.
Notes: Polyester resin plastics products fabrication entails laying reinforcements such as glass fiber in a mold and saturating it with a polyester plastic resin.
The resin hardens to form a rigid plastic part, reinforced with the fiberglass.
The resin is mixed with a catalyst as it is applied that causes a cross-linking reaction between the resin molecules.
Cross-linking reaction causes the resin to harden from a liquid to a solid.

## Slide 64
Let’s Discuss Fabrication With FRP

## Slide 65: Fabrication With FRP
Fabricating with Metals : Structure is Produced & External Paint is Applied
Fabrication with FRP : Reverse
Start with Mold
Pigmented Polyester Coating (Gel Coat) is Applied to the Mold
Structural Reinforcement is Built Using Fiber Glass & Polymer Resin
Finished Part is Removed from Mold
Notes: Room Temp. is used in :
Casting and Laminating applications

## Slide 66
First Step : Mold
Notes: Open Mold
Fiberglass boat parts are built :
“from the outside in”
Resin & Gel Coats containing STYRENE are also used to make these boat molds

## Slide 67
Second Step:
Wax Application

## Slide 68
Gel Coat Applied to Mold
Notes: The Mold is sprayed with a layer of Gel Coat
Gel Coat : Pigmented polyester resin that hardens and becomes the smooth outside surface of the boat
Fiberglass boat parts are built :
“from the outside in”

## Slide 69
Chopped Fiberglass Application
Notes: The inside of the hardened gel coat is coated with a “skin coat” of :
1. Chopped glass fibers and
2. Polyester or vinyl ester resin
Resin acts like a binder or a cementing constituent

## Slide 70
Chopped Fiberglass Application

## Slide 71
Chopper Gun
Notes: Chopper Gun (Fiberglass, resin and catalyst are sprayed together)

## Slide 72
Notes: Finished top half

## Slide 73
Gel Coat Application : Spray Booth
Notes: The lower half is sprayed with a layer of Gel Coat in a spray booth

## Slide 74
Gel Coat :
Spray Booth

## Slide 75
Gel Coat Applied to Mold
Notes: Layer of Gel Coat left to cure at room temp.
TQ#13
Types of Gel Coats Used in Boat Mfg Ops:
Clear gel coat
Pigmented gel coat
Tooling gel coat
TQ
13

## Slide 76
Fiberglass Reinforcements
Notes: Additional layers of fiberglass cloth saturated with resin are added until the final thickness is achieved

## Slide 77
Saturating with Resin
Notes: Promoters, Inhibitors and Accelerators are used to adjust the gel time of the curing reaction
Fillers such as silica, silicon carbide and ceramic beads are added for electrical insulation or abrasion resistance.

## Slide 78
Curing Process
Notes: Reinforced fiberglass cloth saturated with resin allowed to cure
Cure can be caused by :
 Cross linking agents
 With or without Catalyst
 With or without Heat

## Slide 79
Curing Process

## Slide 83
Notes: Boat Interiors : Carpeting and fabric is mostly bonded with contact adhesives.
Contact adhesives contain HAPs :
Methylene Chloride
Toluene
Xylene
Methyl Chloroform
Emissions from these compounds need to be included in all calculations!
TQ
4

## Slide 84
Assembly Line
Notes: Large Boat Manufacturing Facility
HAP Source >> MACT Source (EPA NESHAP)
MAJOR SOURCE (HAP) DEFINITION :
PTE of 10 tons/year or more of any single HAP or
25 tons/year or more of multiple HAPs
TQ
2

## Slide 85
Finished Product

## Slide 86
Let’s Discuss
Fabrication of
Cultured Stone

## Slide 87
Types of Cultured Stone
Cultured Marble
Cultured Granite
Cultured Onyx

## Slide 88: Cultured Marble
Consists of 
  Crushed Marble & Stone (Mined)
  High Strength Polyester Resin
  Protective Gel Coat on the Surface
Mixture is Poured into a Mold
Allowed to cure and shrink
Part is trimmed and polished
Notes: Artificial Marble Production
It is used with 70-80% transparent fillers (Dolomite, Limestone, Aluminum Hydroxide, Silica Sand and Quartz) to obtain polyester marble and plain colored sanitary products.
Without filler it is used in the production of souvenir goods and jewelry. It can be used as an laminating resin when fast curing is not necessary.
CONSISTS OF: Crushed Marble & Stone (mined)
High Strength Polyester Resin
Protective Gel Coat
TQ
5

## Slide 89
Protective
Gel Coat

## Slide 90
Fabrication of Cultured Marble

## Slide 91
Cultured
Marble
Products
Notes: Vanity tops, dressing table tops
Drop-in sinks, tops for drop-in sinks
Pedestal sinks

## Slide 92
Trimming & Polishing

## Slide 93
Cultured
Marble
Product

## Slide 94: Cultured Onyx
Consist of 
  Alumina Trihydrate
  Polyester Resin Content 28 - 35%
  Protective Gel Coat on the Surface
Products are translucent
They have an added visual depth or a 3-D effect
Notes: Cultured Onyx →→→ Generally have an added
visual depth or 3-D effect

## Slide 95
Cultured Onyx Product

## Slide 96: Cultured Onyx Product
Consists of 
  Crushed Stone & Mineral Chips
  Polyester Resin Content 40%
  Protective Gel Coat
Offers the Beauty of Quarried Granite
Low Cost
Stain Resistant Coating
Notes: Cultured Granite
Consists of 
  Crushed Stone & Mineral Chips
  40% Polyester Resin
  Protective Gel Coat
    Transparent
    Durable
Advantages of 
  Beauty of Quarried Granite
  Low Cost
  Stain Resistant Coating

## Slide 97
Crushed Stone

## Slide 98
Polyester Resins

## Slide 100
Curing Process

## Slide 101
Cultured Granite

## Slide 102
Let’s Discuss Open
Molding Operations

## Slide 103: Process and Control
Types of Open Molding Operations
  Hand lay-up & Spray-up
  Pultrusion
  Filament winding
  Casting or molding
  Infusion or scrimp
Notes: Open Molding
Process of laminating a gel coated mold
Atmospheric conditions
Using resin & fiberglass
Hand lay-up or Spray-up
Generally speaking, Open Mold Systems produce higher levels of VOC & HAP emissions than other molding operations.
TQ
24

## Slide 104: Hand Lay-Up
Simplest Type/Very Flexible
Apply Gel Coat, Resin, Fiberglass by Hand
Roller or Brushes Used for Resins
High Strength to Weight Ratio
High Styrene Emissions
Suitable for Prototypes & Low Volume Production
Notes: Also called Contact Molding
Production technique suitable for :
1. Prototypes and
2. Low volume production of fiber composite material parts.
The composite part will have a :
 nice smooth surface on one side and
 very rough one on the other

## Slide 105
Notes: The fibers are manually placed into a one-sided gel coated male or female mould.
A matrix of thermosetting resin is rolled onto the fibers using an hand roller.
More layers can be added
After drying, the composite part can be removed from the mould.

## Slide 106
Hand Lay-Up

## Slide 107
Examples of Hand Lay-Up Operations

## Slide 108
Hand Lay-Up Product
Notes: FB 117 Stealth Fighter
Aircraft wing : The wings of this fighter are produced of carbon reinforced epoxy, by manual fiber molding, followed by autoclave injection molding.
The material has been chosen for its low weight and good strength.

## Slide 109
Let’s Discuss Hand Lay-Up Product :
Surfboard Manufacturing

## Slide 110
First Step :
Foam Core
Notes: Polyurethane Foam core:
Provides buoyancy

## Slide 111
Foam Core :
Shaping & Sizing

## Slide 112
Fiberglass
Surfacing
Mat

## Slide 113
Fiberglass & Resin
Applied to Core
Notes: Resin is allowed to cure.
Polyester Resin → Wicking Resins
→ Resin will continue moving along fibers
Epoxy Resin → Gap-Filling Resins

## Slide 115
Fiberglass & Resin Application

## Slide 116
Grinding & Sanding
Operation

## Slide 117
Grinding &
Sanding
Tools

## Slide 118
Waxing & Coating
Operation

## Slide 120
Curing Operation

## Slide 121
Let’s Discuss Carbon Fiber Epoxy Resin Mfg.

## Slide 122
Bicycle Frame
Components

## Slide 123
Carbon Fiber
& Mold

## Slide 124
Top & Bottom
Half of Mold
Notes: Frame is cured by placing it in a strong magnetic field !!
Computer controlled.
20020084629 Army Research Lab., Weapons and Materials Research Directorate, Aberdeen Proving Ground, MD USA
Induction Bonding for Structural Composite Tubes Final Report, Sep. 2000-Aug. 2001
“Large structural composite tubes, prototype components for a proposed U.S. Navy application, are bonded by induction curing of an engineering adhesive. Magnetic powder is used as the susceptor material and is directly incorporated into the adhesive prior to processing. Different induction power supplies, coil designs, and adhesive formulations are investigated. Final demonstration runs bond 9-in-long, 3-in-diameter axisymmetric bondlines in 15 min. These results demonstrate for the first time the successful induction bonding of large structural composite components using magnetic particulate susceptors.”

## Slide 125
Bicycle Frame :
After Curing Process

## Slide 126
Spray Painting
Operation

## Slide 127
Bicycle Frame : Finished Product

## Slide 128: Spray-Up
Versatile Process
Cost Effective Method of Producing Large Open-Molded Parts
Chopped Fiberglass is Sprayed With
 Catalyzed Resins onto Gel Coat
 Compacted

## Slide 129
Spray-Up

## Slide 130: Spray-up

## Slide 131
Chopped Fiberglass Spray-up Operation

## Slide 132
Controlled Spraying
Reduces styrene emissions
Increases transfer efficiency
Low fluid tip pressure
Employee gun handling training
Close containment flanges
Notes: CONTROLLED SPRAYING OPERATIONS
    Reduces styrene emissions
    Increases transfer efficiency
    Low fluid tip pressure
    Employee gun handling training
    Close mold flanges
[Mold flanges surround the edge of a mold. Close mold flanges help to minimize spray off mold edges.]

## Slide 133
Gel Coat Application

## Slide 134
Gel Coat Application in a Spray Booth
Notes: Polyesters release heat when they cure.
 exothermic reaction
If the casting gets too hot :
 Degrade  Bubble
 Turn brown  Crack
This generally limits the thickness of castings to less than 1/4" thick layers.

## Slide 135
Gel Coat Storage

## Slide 136: Approved Spray Guns
High Pressure Airless Guns
Air-Assist Airless Guns
Electrostatic Spray
High Volume Low Pressure (HVLP) 
Fluid Impingement Technology (FIT) Spray Gun 
Notes: APPROVED SPRAY GUNS
High Pressure Airless Guns
Air-Assist Airless Guns
Electrostatic Spray
High Volume Low Pressure (HVLP) 
Fluid Impingement Technology (FIT) Spray Gun 

## Slide 137
HVLP Spray Gun
Notes: HVLP Spray Gun
0.1 to 10 psig (Some agencies define as)
Provides high transfer efficiency of materials
Shown:
Resin hose
Catalyst hose
Air pressure hose
TQ
22

## Slide 138
Fluid Impingement Technology Spray Gun
Notes: Ways to Reduce VOC Emissions
Increases transfer efficiency
FIT spray guns : $2,500
Higher transfer efficiency than HVLP
Being evaluated as BACT

## Slide 139
Let’s Discuss other Open Molding Operations

## Slide 140: Pultrusion
Pulled extrusion process
Fiberglass under tension
Immersed in Resin bath or injection
Pulled through forming dye
Pulled through heated dye to cure
Produces flat stock for cutting
VOCs at resin bath and forming area
Notes: This process enables the production of large series of continuos fiber
1. Fibers are pulled through a plastic bath 2. Through a heated die which give the profile its shape
3. Profile is cooled by air or water and cut into desired lengths.
Advantage  Relatively inexpensive way to produce reinforced parts with long fibers.
Strength and other properties are better in the fiber direction than across.

## Slide 141: Pultrusion
Strand Tension Device
Forming Die
Roving
Strands
Resin Bath
Heated
Die
Formed
Impregnated
Strands
Pull Rollers

## Slide 142: Filament Winding Operations
Used in Manufacture of:
  large pipes and storage tanks
  hollow vessels subject to high internal pressure
Strand Rovings are Pulled under Tension into a Resin bath
Wound into Shape & Cured
Notes: Generally limited to Cylindrical shells
High strength to weight ratio achieved
Underground gasoline storage tanks
High pressure lab gas bottles

## Slide 143
Filament Winding
Notes: Moderate VOC emissions from low resin viscosity

## Slide 144
Let’s Discuss Closed Molding Operations

## Slide 145: Resin Transfer Molding
Gel Coat is Applied to Mold
Reinforcing Fibers are Placed into the Mold Cavity
Mold Halves are Closed & Clamped
Liquid Resin is Injected into the Mold Cavity
 Suitable for High Vol. Production
 Reduced VOC emissions
Notes: 1. Gel coat is applied to the mold
2. Mats of reinforcement material are placed in a mold which is then closed.
3. Resin is injected into the mold.
4. After hardening the finished part can be removed from the mold.
The process is used where advanced geometry is required, and for car parts.

## Slide 146: Resin Transfer Molding
Resin
Top Mold
Mat
Bottom Mold
Notes: RTM produces strong fiber reinforced parts of thermosetting plastics with smooth surfaces on both sides.
Plastic parts with different separated colors or materials are produced using this process. Injection molding.
1. One element of the part is molded.
2. A section of the tool is replaced leaving a new cavity
3. Next color or component can be molded embedding the first one.

## Slide 147
Notes: Blow Molding
Used for hollow parts of all sizes.
1. A tube of molten plastics is extruded into an open mold.
2. The mold closes and thereby the bottom of the part welds.
3. Hot air is blown into the tube and it is blown up until it fills out the mold cavity.
Production in small and large quantities :
 Setup cost is low

## Slide 148
Notes: Gas Assisted Injection Molding
Used for high quality bottles like bottles for mineral water containing CO2 under pressure.
Compared to blow molding, injection blow molding gives better definition of details (e.g. screw thread), and a better control of the distribution of the thickness of the material.

## Slide 149
Notes: Injection Molding

## Slide 150
Let’s Discuss Emissions & Controls

## Slide 151: Emission Sources
Gel coat - Styrene Emissions
  Application (atomization)
  Curing
Resin
  Styrene most common monomer
Mixing
Clean-up solvents

## Slide 153: Process Materials
General Purpose Resins : 35% styrene
Specialty Resins : <50% styrene
Most AQMD Rules : 35% styrene
Tough Low Profile Resins <35% styrene
  Higher viscosity
  Need better surface prep
  Need good wet-out procedures
Notes: TQ
6

## Slide 154: Solvents
Acetone (widely used)
Methyl Ethyl Ketone (MEK)
Dibasic Ester (DBE)
- less volatile, less flammable than acetone
Water-based resin emulsifiers
- detergent cleaners
Notes: MACT Requirements
Boat manufacturers must use solvents with < 5% air toxic content for →→
→ routine cleaning of resin and gel coat application equipment
In the Past Solvents used for surface preparation & equipment cleaning
were generally HAPS
TQ
3

## Slide 155
Open Acetone Container

## Slide 157: Clean-Up Rules
  Cleaning with Compounds 50 to 200 g/liter VOC
  Closed containers
  Self-Closing Containers
  Styrene soaked rags in closed containers
Notes: California agencies limit VOC to 50-200 g/liter
HAP containing solvents are used to clean :
1. Surface before finishing
2. Paint and coating spray guns
Many operations use chlorofluorocarbons (CFCs) many of which are exempted by the federal definition of VOC.
TQ
16

## Slide 158
Open Containers

## Slide 159
Potential Emissions??

## Slide 160
Let’s Discuss Styrene Emissions

## Slide 161: Styrene : HAP Source
Unsaturated aromatic HC
Petroleum By-Product
In Polyesters :
 Reactive Diluent
Styrene : HAP (Hazardous Air Pollutants)
Notes: Primary VOCs in gel coats is from: Styrene
Styrene serves as a reactive monomer
It chemically reacts with the base polymer as part of the curing process.
EPA has identified boat manufacturing as a major source of HAPs, such as Styrene.

## Slide 162: Styrene : HAP Source
Foamed or Expanded Polystyrene:EPS
Exceptional insulation properties
Foam cups & containers
Foodservice products
Packaging & protecting
Notes: Foamed or Expanded Polystyrene : EPS
Exceptional insulation properties
Foam cups & containers
Foodservice products
Packaging & protecting

## Slide 163: Styrene Emissions Determination Models
A 540 lb. Drum of Gel Coat
 38% VOC
 Applied by “Uncontrolled Spray” Techniques
 Emit 100 lb. of Emissions
Two Drums of Gel Coat/day
 25 Tons of Emissions/Yr
Notes: Using Unified Emissions Factors for Open Molding of Composites
Table for 38% styrene gel coat gives 398 as emission factor
(398 lb/ton) x (540/2000 tons) = 107.5 lb styrene emissions per day
A source using one drum per day of this gel coat would have emissions greater than 10 tpy and would be a major source!
A 04 0:49:00

## Slide 164
Notes: Styrene is the primary raw material from which Polystyrene is made.
In fact, approximately 50% of the styrene produced is used in the manufacture of Polystyrene products.
TQ
17

## Slide 165
Let’s Discuss VOC Control

## Slide 166: Control of VOC Emissions
Process change to control monomer emissions
Low VOC Gel Coat
Change from acetone to less volatile solvent
Reclaim acetone (distill)
ADD-ON equipment
Notes: New lower-emitting resins and gel coats
1/4 to 1/3 of total gel coat emissions can be reduced by using a Low VOC gel coat
 emissions per part =  parts produced under the same permit
 Styrene gel coat  Low VOC gel coat
(other VOCs substituted for Styrene)
MMA (Methyl Methacrylate)

## Slide 167: Add-On Control Methods
Incineration
Absorption
Adsorption
Condensation
Notes: Note: Overview slide. Will cover all areas in-depth.

## Slide 168
Thermal Oxidizer/Afterburner
Notes: Sometimes referred to as “INCINERATORS”
VOC air stream is heated to high temp.
VOC Oxidized  H2O & CO2
Residence Time : 0.5 sec
General operating temperature  1400 F
Thermal Oxidation Principle : 3 T’s
Heat Exchangers pre-heat inlet gas stream less fuel
Inlet VOC streams for safety are maintained at 25% of the Lower Explosive Limit (LEL)
LEL is the concentration at which a VOC will explode if exposed to an ignition source. An example (not recommended to do but has been observed): A cigarette can be extinguished in gasoline. The concentration is to high (not enough oxygen/air to allow combustion), above the upper explosive limit.
QUESTION: “Can a BOILER be used as an INCINERATOR?”
ANSWER: Yes, frequently a boiler can be used to burn captured and waste organics. An example would be pentane gas used in an expandable polystyrene blowing operation.
TQ
14

## Slide 169
Thermal Incinerator
Notes: This is an example of a typical thermal oxidizer
 Used for abatement of VOCs & Toxics

## Slide 170
Venting to Oxidizer

## Slide 171
Auxiliary Fuel Burners
Optional Heat Recovery
Catalyst Bed
Waste Gas
Stack
Catalytic Oxidizer/Incinerator
Notes: Catalytic oxidizers operate at lower temps
than thermal oxidizers
600-800 F
Platinum DISADVANTAGE:
Palladium All of which can be
Copper Oxide fouled or blinded by
Chromium contamination.
Cobalt
Ceramic Materials
Catalysts dispersed in thin layers
to provide for maximum surface contact
POINT OF INSPECTION: Visible
emissions may indicate poor burner
operation or condensation of unburned
organics.
TQ
20
TQ
12

## Slide 172
Notes: Discuss bypass around control equipment
TQ
20
TQ
12

## Slide 173: Wet Scrubber
Notes: This is a B & W wet FGD scrubber
 Divided into 4 distinct regions:
1) Quenching : saturates & cools the flue gas
2) Absorption : gas rises through a distribution tray, contacting a froth of slurry
3) Moisture Separator : prevents slurry carryover and corrosion and deposits downstream
4) Tank Agitation : to keep the solids in suspension

## Slide 174
Carbon Adsorption System
Filter
Vapor-Laden Air Stream
Cooler
Fan
Low-Pressure Steam
Adsorber 2
Adsorber 1
Control Device
Air Stripped
Notes: Carbon adsorption :
Can be used w / Low VOC concentrations
Organic compounds in gas stream - weakly adsorbed - surface of activated carbon
(very high surface area / gram of material)
Dual Beds usually used. When one bed is nearly saturated - effluent stream switched to other bed
Type, amount, and granular size of the carbon used is dependent on the type of contaminant and its concentration
“Working Bed Capacity” - generally 25% to 50% of the maximum capacity of the carbon
“Breakthrough” - occurs when the mass transfer zone reaches the end of the carbon bed.
TQ
21

## Slide 175: Remediation System with Carbon Adsorbers
Notes: Fouling from high MW monomers
Acetone reduces efficiency
PM clogging

## Slide 176
Regulatory Requirements
Notes: MACT standards generally apply only to :
“Major Sources” – both new and existing
Boat manufacturers will have the flexibility to comply by :
 Averaging air toxics contents of materials used …..
…….. within a single operation or among several resin and gel coat operations.

## Slide 177: Regulatory Requirements
Federal, state, and local requirements
Resin specific limits
Permit requirements
Monitoring requirements
Visible emission limits
Nuisance regulations
Breakdowns & variances.

## Slide 178: Federal Regulations
1990 Clean Air Act
  NESHAPS : National Emissions Standards for Hazardous Air Pollutants
  HAPS : Hazardous Air Pollutants
  MACT : Maximum Achievable Control Technology
  New & Existing Major Sources
Notes: In 1990, Congress modified the Clean Air Act
A number of chemicals were classified as HAPs.
Many of the HAPs are also VOCs (Styrene)
EPA proposed MACT standards to regulate emissions for a number of products and processes, including HAPs
MACT standards generally apply only to :
“Major Sources” – both new and existing
Emissions from gel coat spray applications are significant
TQ
7

## Slide 179: Federal Regulations
40 CFR Part 63 Subpart VVVV -- NESHAP for Boat Manufacturing
40 CFR Part 63 Subpart MMMMM -- NESHAP for Flexible Polyurethane Foam Fabrication
40 CFR Part 63 Subpart U -- NESHAP for
Group I Polymers & Resins
40 CFR Part 63 Subpart JJJ -- NESHAP for
Group IV Polymers & Resins
Notes: Purpose of NESHAPs :
To Protect public health by reducing emissions of Hazardous Air Pollutants (HAPs) from various operations.
VVVV -- covers resin and gel coat operations at fiberglass boat manufacturers, paint and coating operations at aluminum boat manufacturers, and carpet and fabric adhesive operations at all boat manufacturers.
WWWW : REINFORCED PLASTICS COMPOSITES PRODUCTION -- covers manufacturing of reinforced and non-reinforced plastic composites or plastic molding compounds using thermoset resins and/or gel coats containing styrene. (Also: cleaning, mixing, storage and repair.)
MMMMM -- covers slabstock, molded and rebond flexible polyurethane foam production. Products include: furniture seat cushions and bedding materials; automotive seats, packaging and a wide variety of specialty products; and carpet padding and cushions for school bus seats.
U – covers elastomers used to produce a variety of synthetic rubber products, including tires, hoses , belts, footwear, adhesives, caulks, wire insulation, seals, floor tiles, and latexes.
JJJ – covers manufacturing of terephthalates polymers and certain styrene-based thermoplastics which are used to produce such products as polyester fibers, soft drinks bottles, automotive plastic parts, packing materials and plastic toys.
TQ
1

## Slide 180: Federal Regulations
63 WWWW – Reinforced Plastics Composites Production
63 III – Flexible Polyurethane Foam Production
63 6O – Area Source Flexible Polyurethane Foam
63 YY – Generic MACT Acetal Resins, Polycarbonate, etc.
63 W – Group II Polymers and Resins
63 OOO – Group III Polymers and Resins
63 6L – Area Source Acrylic and Modacrylic Fiber Production
63 7H – Polyvinyl Chloride and Copolymers Production
63 6D – Area Source Polyvinyl Chloride and Copolymers
63 4H – Wet Formed Fiberglass Mat
60 HHH – NSPS for Synthetic Fiber Production
60 VVV – NSPS for Polymeric Coating for Supporting Substrates
Notes: IMPORTANT NOTE:
Subpart WWWW applies to the production of both reinforced and NON-reinforced plastics “located at
a major source of HAP emissions and that uses thermoset resins and/or gel coats that contain styrene.”
TQ
1

## Slide 181
Notes: Mark Morris
EPA's Office of Air Quality Planning and Standards
(919) 541-5416.

## Slide 182
BACT and BARCT
Notes: Synthetic Marble Casting has lower BACT standards
They are :
 General Purpose Resins < 30%
   Pigmented Gel Coats < 35%
   Clear Gel Coats < 47%
Closed Molding has lower BACT standards
   Resins < 28%
Please note that the styrene content of Specialty Resins is higher that the General Purpose Resins.
TQ
6

## Slide 183: Typical Permit Conditions
Daily Emissions Limits
Gel Coat Monomer Content (weight %)
Resin Monomer Content (weight %)
Amount of Material Used
Cleaning Material
Logs
Notes: [cover San Joaquin Permit to Operate]
  Daily Emissions Limits
  Gel Coat Monomer Content (weight %)
  Resin Monomer Content (weight %)
  Amount of Material Used
  Cleaning Material
  Logs

## Slide 184
Inspection Procedures

## Slide 185: Reasons for Inspections
Compliance determination
Complaint investigation
Source plan approval
Review or renewal of permits
Special studies.
Notes: Examples of special studies would be :
 Operating and maintenance evaluations
 Updating emission inventories

## Slide 186: Pre-Inspection
Prepare inspection report form
File review
Regulation review
Equipment check
Pre-entry & entry
Pre-inspection meeting
Permit check.
Notes: Prior to the site inspection the inspector should review all information available in the district source files including: approved permits, equipment lists, conditions for each permit, previous inspection reports, Notices of Violation, breakdown reports, enforcement actions taken, odor complaints, variance histories, alternative emissions control plans, abatement orders, source tests, and the design of the plant.
Verify that all applicable permits for the facility are current and valid. Bring a current copy of the permit(s) and bring extra copies in case the facility has misplaced or lost their copy.
The inspector may wish to complete some portions of the inspection documentation before arriving at the facility as this will save time during the pre-inspection meeting. If your district has checklists or rule specific inspection forms, use them.
You should review any references to the specific rules which are noted in the source files. In particular, be familiar with each standard and exemption in the rules. Discuss regulations that apply to the facility with experienced personnel
TQ
18

## Slide 187: Inspection
Visible emission evaluation
General upkeep & maintenance
Maintenance records
Operational records
Any open containers?
Self-closing containers
Rags and waste in closed containers
Notes: Make sure that you have the proper safety equipment available for use during the inspection. When you arrive at the plant, notice if there are any visible emissions. If there are any visible emissions, make sure you document them and plan on finding the sources as soon as possible after entering the facility.
Request to see the previous contact mentioned in the files. Depending on the facility, it may be the environmental coordinator, supervisor, president, maintenance worker or operator. Always present your business credentials immediately to avoid confusion.
If the source is unfamiliar with your district’s authority be prepared to cite and provide copies of California Health & Safety Code (CHSC) Section 41510: Right of Entry. Know and follow your district’s policy if the facility refuses entry.
Before the inspection begins the inspector should meet with the source representative to obtain operating information. The inspector should state the purpose of the inspection and identify the equipment which will be inspected. Facility information can be verified during this meeting including: the facility name and ownership, address complete with city and zip code, contact name, contact title, phone number and area code. Discuss safety procedures and whether or not there have been any problems in the past. Request a copy of applicable material safety data sheets (MSDS). If necessary discuss sampling procedures with the source representative. Check existing permit conditions and ask if any other changes have been made to the operation which are not reflected in the permit.
Following the inspection the inspector should confer with the source representative on the findings and issue warnings, violations, etc.
TQ
18
TQ
19

## Slide 188
Closed Containers

## Slide 189
Open
Container

## Slide 190
Potential
Emissions??

## Slide 191
Catalyst (MEKP)
Emissions

## Slide 192
Closed Paint Containers

## Slide 193: Inspection
Coating Application Equipment
VOC content of solvents and other chemicals
MSDS
Spray Booths
Dust control equipment
  Filters and screens
  Cleaned as often as necessary

## Slide 194
Compliant
Spray Gun

## Slide 195
Spray
Booth

## Slide 196
Spray Booth Filters

## Slide 197
Filter Inspection

## Slide 198
Inspector Safety
Proper equipment
Plant evacuation
Inhalation hazards
Hazardous materials
Chemicals & Machinery

## Slide 199
Questions