## Slide 1
PLASTIC RESINS AND FIBERGLASS OPERATIONS
NACT Course 261

## Slide 2
OZONE Formation

## Slide 3
Plastic resin uses
Plastic resin theory / operation
Air pollution control devices
Implementing regulations
Typical permit conditions
Inspection procedures
Federal regulations
Course Overview
Notes: Stated as objectives, upon completion of this course, you should:
Be familiar with some industrial uses of plastic resins.
Using appropriate terminology, be able to explain the theory of operations of polyester and epoxy resins.
Be able to describe the major methods and devices used in controlling air contaminant emissions from polyester resin operations.
Be familiar with some of the implementing HAP emission control regulations.
Be familiar with some typical polyester resin permit conditions.
Be able to explain how to conduct an inspection of a polyester resin operation.

## Slide 4: Uses of Polyester Resins
Aircraft / Aerospace / Automotive
Marine / Railroad applications
Electrical / Electronic components
Construction / Building materials
Packaging materials
Consumer / Institutional products
Corrosion resistant products
Business equipment
Furniture / Furnishings

## Slide 5
Composite Decking

## Slide 6
Structural strength & rigidity
Heat resistance
Corrosion resistance
Dielectric strength
Design flexibility
Low finish cost
Moisture resistance
Reuse & recycle
Light weight
Durable
Advantages

## Slide 7: Disadvantages
VOC emissions
Toxicity issues
Flammability
Storage
Disposal

## Slide 8: Emissions From Polyester Resins
Ethylene
Styrene / MMA
Ethylene Glycol
Pentane
Acetone / MEK
MEKP
Dibasic Ester
Resins
&
Glass
Fiber
Notes: TQ
15

## Slide 9
Plastic
  Organic compounds that can be molded
Polymer
  Two or more like molecules joined to form a more complex, physically different molecule
Resin
  Carbon compound polymers used in reinforced products to surround and hold fibers
Common Terms

## Slide 10
Consist of building blocks : HC
  Derived from petroleum or NG
  Monomers (mono=one, mer =unit)
  Bonded into chains  Polymers
Reaction known as Polymerization
  Ethylene  Polyethylene
  Propylene  Polypropylene
How are Plastics made?

## Slide 11
Let’s Discuss Common Plastics

## Slide 12
Polycarbonate
Polyethylene
Polystyrene
Polypropylene
Polyurethane
Polyvinyl Chloride
Polyesters
Common Plastic Materials

## Slide 13
Created to compete with die-cast metals
Strong, tough & rigid
Excellent electrical insulators
Mostly electrical uses
Polycarbonates

## Slide 14
Clear, very tough polymer
Excellent barrier against O2 and CO2
Good chemical resistance
Soft drink bottles
Fiber (the polyester 70s!!!)
Magnetic tape (audio & video)
Polyethylene : PET

## Slide 15
Polyester Fiber Jacket

## Slide 16
Fleece Made From
Recycled “PET”

## Slide 17
PET
Product

## Slide 18: High Density Polyethylene
High density version of PE
Excellent protective barrier properties & Strong
Milk, juice & H2O container
Household chemicals
Detergents

## Slide 19
High Density
Polyethylene

## Slide 20: Low Density Polyethylene
Low density version of PE
Offers clarity & flexibility
Provides ductility
Grocery & garbage bags
Shrink & stretch films

## Slide 21
Composite Decking

## Slide 22: Polypropylene
“Workhorse” of plastics
High tensile strength
High melting point
Good chemical resistance
Packaging & carpeting
Automotive & appliances

## Slide 23
Foamed or Expanded Polystyrene : EPS
Exceptional insulation properties
Foam cups & containers
Foodservice products
Packaging & protecting
Polystyrene

## Slide 24
Expanded Polystyrene
Foam

## Slide 25
Recycled Polystyrene

## Slide 26
Recycled Polystyrene
Baseboard Molding

## Slide 27
Foam : bedding, auto seats, cushioning, carpet underlay
Insulation & flotation
Polyurethane coatings
Abrasion resistant : printing rolls, conveyor belts, gaskets & seals
Polyurethanes

## Slide 28
Polyurethane
Foam

## Slide 29: Polyvinyl Chloride (PVC)
Chemical, abrasion & weather resistance
Pipes & sidings
Leather-like upholstery
Gloves, boots & apparel

## Slide 30
What are Composites?

## Slide 31: Introduction to Composites
Made up of 2 or more components
  Fibrous reinforcing network embedded in the cured resin matrix
  Types of reinforcements
   Fiberglass, Carbon fiber & Kevlar
  Thermosetting type resin is a plastic that cures from a liquid to a solid state
   Polyester, Vinyl, Epoxy & Urethane
Notes: TQ
11

## Slide 32
Composite
Material

## Slide 33
Types of
Reinforcements
• Fiberglass
• Carbon Fiber
• Kevlar

## Slide 34: Carbon Fiber
Stiffest & strongest reinforcing fibers for polymer composites
Used together with epoxy
Race cars
Space applications
Sporting equipment

## Slide 35
Carbon Fiber

## Slide 36
Carbon Fiber

## Slide 37
Carbon Fiber Product

## Slide 38
Made of silicon oxide
Produced by a spinning process
Pulled through a nozzle from molten glass
Reinforcing materials
Automotive and naval industries, sporting equipment
Fiberglass
Notes: TQ
10

## Slide 39
Fiberglass Forms

## Slide 40: Fiberglass Forms
Surfacing Mat (Veil)
Chopped Strand Mat
Roving (Spool)
Woven Roving
Cloth (Hand Lay-up)

## Slide 41
Fiberglass
Forms

## Slide 42
Fiberglass
Forms

## Slide 43
High strength
Low price
Dimensional stability
Temperature resistance
Corrosion resistance
Low weight
Excellent dielectric properties
Fiberglass Advantages

## Slide 44
Fiberglass Product

## Slide 45
Fiberglass
Spa

## Slide 46: Types of Fiberglass
E-glass and S-glass
  E-glass  Good electrical properties
  S-glass  Very strong, stiff, and temperature resistant

## Slide 47: Glass Fiber Reinforced Resin
Most used composites
Temp resistance & strength
Impregnating fibers with liquid epoxy resins
Aircraft components
Casings for missiles, pipes, tanks, pressure vessels

## Slide 48: Kevlar
Lightweight Flexible Comfortable
High Tensile Strength
Excellent Dimensional Stability
High Flame Resistant
High Chemical Resistant
Used with epoxy or vinyl resin

## Slide 49
Kevlar Product

## Slide 50
Protective & Performance Apparel
Composites : aircraft parts/boats
Fiber-Optic Cables
Tires
Ropes & Cables
Brake Pads & Clutch Linings
Power Transmission Belts / Hoses
Kevlar

## Slide 51
Kevlar
Product

## Slide 52
Let’s Discuss Types of Plastic Materials

## Slide 53: Types of Plastic Materials
Thermoplastic Resins
  Become fluid upon heating
  Repeatable & reversible process
  No chemical change
  No permanent change in physical prop.
  Readily extruded or molded
  E.g.. film, fibers, bottles etc.
  Polyethylene, Polystyrene & Polypropylene
Notes: TQ
23

## Slide 54: Types of Plastic Materials
Thermosetting Resins
  Irreversibly polymerizes and solidifies
  Chemical structure permanently altered
  Cannot be resoftened
  Process called curing or hardening
  E.g.. Molding, casting, powder coating
  Polyurethanes, Polyester & Epoxy resins

## Slide 55: Thermoplastic vs. Thermosetting
Thermoplastic Thermosetting
Faster molding Design constraints
Lower emissions Limited unit production
Lower costs Performance requirements Easy recycling Market demands
Low labor intensity

## Slide 56
Resins Fiberglass
Fiber substrate Catalysts
Additives Solvents
Initiators
Raw Materials

## Slide 57
Typical Raw Materials

## Slide 58
What is a Resin?

## Slide 59: Thermoset Resins
Two Common Types
 Epoxy & Polyester
 Molding, Laminating, Casting ….
  Epoxy
   Higher Performance & Higher Price
   High Strength, Weight Critical
   Dimensionally Accurate Applications

## Slide 60
Epoxy
Resin
Product

## Slide 61: Polyester Resins
Building Blocks for Polyester Resins
Acids & Glycols Cooked Together
Dissolved in Styrene Monomer
Inhibitors Added to Delay Reaction
Product Added to a Peroxide Catalyst
    Unsaturated Portions of Monomer and Polyester React Together
Hard Solid Mass

## Slide 62
Polyester Resins

## Slide 63: Fabrication With Polyesters
Reinforcements such as a Glass Fiber in a Mold
Saturated with Polyester Resin
Resin Mixed with Catalyst Causing Crosslinking Reaction
This Causes Resin to Harden from Liquid to Solid
Polyester Resin in Fiberglass Boat Mfg.

## Slide 64
Let’s Discuss Fabrication With FRP

## Slide 65: Fabrication With FRP
Fabricating with Metals : Structure is Produced & External Paint is Applied
Fabrication with FRP : Reverse
Start with Mold
Pigmented Polyester Coating (Gel Coat) is Applied to the Mold
Structural Reinforcement is Built Using Fiber Glass & Polymer Resin
Finished Part is Removed from Mold

## Slide 66
First Step : Mold

## Slide 67
Second Step:
Wax Application

## Slide 68
Gel Coat Applied to Mold

## Slide 69
Chopped Fiberglass Application

## Slide 70
Chopped Fiberglass Application

## Slide 71
Chopper Gun

## Slide 73
Gel Coat Application : Spray Booth

## Slide 74
Gel Coat :
Spray Booth

## Slide 75
Gel Coat Applied to Mold
Notes: TQ
13

## Slide 76
Fiberglass Reinforcements

## Slide 77
Saturating with Resin

## Slide 78
Curing Process

## Slide 79
Curing Process

## Slide 83
Notes: TQ
4

## Slide 84
Assembly Line
Notes: TQ
2

## Slide 85
Finished Product

## Slide 86
Let’s Discuss
Fabrication of
Cultured Stone

## Slide 87
Types of Cultured Stone
Cultured Marble
Cultured Granite
Cultured Onyx

## Slide 88: Cultured Marble
Consists of 
  Crushed Marble & Stone (Mined)
  High Strength Polyester Resin
  Protective Gel Coat on the Surface
Mixture is Poured into a Mold
Allowed to cure and shrink
Part is trimmed and polished
Notes: TQ
5

## Slide 89
Protective
Gel Coat

## Slide 90
Fabrication of Cultured Marble

## Slide 91
Cultured
Marble
Products

## Slide 92
Trimming & Polishing

## Slide 93
Cultured
Marble
Product

## Slide 94: Cultured Onyx
Consist of 
  Alumina Trihydrate
  Polyester Resin Content 28 - 35%
  Protective Gel Coat on the Surface
Products are translucent
They have an added visual depth or a 3-D effect

## Slide 95
Cultured Onyx Product

## Slide 96: Cultured Onyx Product
Consists of 
  Crushed Stone & Mineral Chips
  Polyester Resin Content 40%
  Protective Gel Coat
Offers the Beauty of Quarried Granite
Low Cost
Stain Resistant Coating

## Slide 97
Crushed Stone

## Slide 98
Polyester Resins

## Slide 100
Curing Process

## Slide 101
Cultured Granite

## Slide 102
Let’s Discuss Open
Molding Operations

## Slide 103: Process and Control
Types of Open Molding Operations
  Hand lay-up & Spray-up
  Pultrusion
  Filament winding
  Casting or molding
  Infusion or scrimp
Notes: TQ
24

## Slide 104: Hand Lay-Up
Simplest Type/Very Flexible
Apply Gel Coat, Resin, Fiberglass by Hand
Roller or Brushes Used for Resins
High Strength to Weight Ratio
High Styrene Emissions
Suitable for Prototypes & Low Volume Production

## Slide 106
Hand Lay-Up

## Slide 107
Examples of Hand Lay-Up Operations

## Slide 108
Hand Lay-Up Product

## Slide 109
Let’s Discuss Hand Lay-Up Product :
Surfboard Manufacturing

## Slide 110
First Step :
Foam Core

## Slide 111
Foam Core :
Shaping & Sizing

## Slide 112
Fiberglass
Surfacing
Mat

## Slide 113
Fiberglass & Resin
Applied to Core

## Slide 115
Fiberglass & Resin Application

## Slide 116
Grinding & Sanding
Operation

## Slide 117
Grinding &
Sanding
Tools

## Slide 118
Waxing & Coating
Operation

## Slide 120
Curing Operation

## Slide 121
Let’s Discuss Carbon Fiber Epoxy Resin Mfg.

## Slide 122
Bicycle Frame
Components

## Slide 123
Carbon Fiber
& Mold

## Slide 124
Top & Bottom
Half of Mold

## Slide 125
Bicycle Frame :
After Curing Process

## Slide 126
Spray Painting
Operation

## Slide 127
Bicycle Frame : Finished Product

## Slide 128: Spray-Up
Versatile Process
Cost Effective Method of Producing Large Open-Molded Parts
Chopped Fiberglass is Sprayed With
 Catalyzed Resins onto Gel Coat
 Compacted

## Slide 129
Spray-Up

## Slide 130: Spray-up

## Slide 131
Chopped Fiberglass Spray-up Operation

## Slide 132
Controlled Spraying
Reduces styrene emissions
Increases transfer efficiency
Low fluid tip pressure
Employee gun handling training
Close containment flanges

## Slide 133
Gel Coat Application

## Slide 134
Gel Coat Application in a Spray Booth

## Slide 135
Gel Coat Storage

## Slide 136: Approved Spray Guns
High Pressure Airless Guns
Air-Assist Airless Guns
Electrostatic Spray
High Volume Low Pressure (HVLP) 
Fluid Impingement Technology (FIT) Spray Gun 

## Slide 137
HVLP Spray Gun
Notes: TQ
22

## Slide 138
Fluid Impingement Technology Spray Gun

## Slide 139
Let’s Discuss other Open Molding Operations

## Slide 140: Pultrusion
Pulled extrusion process
Fiberglass under tension
Immersed in Resin bath or injection
Pulled through forming dye
Pulled through heated dye to cure
Produces flat stock for cutting
VOCs at resin bath and forming area

## Slide 141: Pultrusion
Strand Tension Device
Forming Die
Roving
Strands
Resin Bath
Heated
Die
Formed
Impregnated
Strands
Pull Rollers

## Slide 142: Filament Winding Operations
Used in Manufacture of:
  large pipes and storage tanks
  hollow vessels subject to high internal pressure
Strand Rovings are Pulled under Tension into a Resin bath
Wound into Shape & Cured

## Slide 143
Filament Winding

## Slide 144
Let’s Discuss Closed Molding Operations

## Slide 145: Resin Transfer Molding
Gel Coat is Applied to Mold
Reinforcing Fibers are Placed into the Mold Cavity
Mold Halves are Closed & Clamped
Liquid Resin is Injected into the Mold Cavity
 Suitable for High Vol. Production
 Reduced VOC emissions

## Slide 146: Resin Transfer Molding
Resin
Top Mold
Mat
Bottom Mold

## Slide 150
Let’s Discuss Emissions & Controls

## Slide 151: Emission Sources
Gel coat - Styrene Emissions
  Application (atomization)
  Curing
Resin
  Styrene most common monomer
Mixing
Clean-up solvents

## Slide 153: Process Materials
General Purpose Resins : 35% styrene
Specialty Resins : <50% styrene
Most AQMD Rules : 35% styrene
Tough Low Profile Resins <35% styrene
  Higher viscosity
  Need better surface prep
  Need good wet-out procedures
Notes: TQ
6

## Slide 154: Solvents
Acetone (widely used)
Methyl Ethyl Ketone (MEK)
Dibasic Ester (DBE)
- less volatile, less flammable than acetone
Water-based resin emulsifiers
- detergent cleaners
Notes: TQ
3

## Slide 155
Open Acetone Container

## Slide 157: Clean-Up Rules
  Cleaning with Compounds 50 to 200 g/liter VOC
  Closed containers
  Self-Closing Containers
  Styrene soaked rags in closed containers
Notes: TQ
16

## Slide 158
Open Containers

## Slide 159
Potential Emissions??

## Slide 160
Let’s Discuss Styrene Emissions

## Slide 161: Styrene : HAP Source
Unsaturated aromatic HC
Petroleum By-Product
In Polyesters :
 Reactive Diluent
Styrene : HAP (Hazardous Air Pollutants)

## Slide 162: Styrene : HAP Source
Foamed or Expanded Polystyrene:EPS
Exceptional insulation properties
Foam cups & containers
Foodservice products
Packaging & protecting

## Slide 163: Styrene Emissions Determination Models
A 540 lb. Drum of Gel Coat
 38% VOC
 Applied by “Uncontrolled Spray” Techniques
 Emit 100 lb. of Emissions
Two Drums of Gel Coat/day
 25 Tons of Emissions/Yr

## Slide 164
Notes: TQ
17

## Slide 165
Let’s Discuss VOC Control

## Slide 166: Control of VOC Emissions
Process change to control monomer emissions
Low VOC Gel Coat
Change from acetone to less volatile solvent
Reclaim acetone (distill)
ADD-ON equipment

## Slide 167: Add-On Control Methods
Incineration
Absorption
Adsorption
Condensation

## Slide 168
Thermal Oxidizer/Afterburner
Notes: TQ
14

## Slide 169
Thermal Incinerator

## Slide 170
Venting to Oxidizer

## Slide 171
Auxiliary Fuel Burners
Optional Heat Recovery
Catalyst Bed
Waste Gas
Stack
Catalytic Oxidizer/Incinerator
Notes: TQ
20
TQ
12

## Slide 172
Notes: TQ
20
TQ
12

## Slide 173: Wet Scrubber

## Slide 174
Carbon Adsorption System
Filter
Vapor-Laden Air Stream
Cooler
Fan
Low-Pressure Steam
Adsorber 2
Adsorber 1
Control Device
Air Stripped
Notes: TQ
21

## Slide 175: Remediation System with Carbon Adsorbers

## Slide 176
Regulatory Requirements

## Slide 177: Regulatory Requirements
Federal, state, and local requirements
Resin specific limits
Permit requirements
Monitoring requirements
Visible emission limits
Nuisance regulations
Breakdowns & variances.

## Slide 178: Federal Regulations
1990 Clean Air Act
  NESHAPS : National Emissions Standards for Hazardous Air Pollutants
  HAPS : Hazardous Air Pollutants
  MACT : Maximum Achievable Control Technology
  New & Existing Major Sources
Notes: TQ
7

## Slide 179: Federal Regulations
40 CFR Part 63 Subpart VVVV -- NESHAP for Boat Manufacturing
40 CFR Part 63 Subpart MMMMM -- NESHAP for Flexible Polyurethane Foam Fabrication
40 CFR Part 63 Subpart U -- NESHAP for
Group I Polymers & Resins
40 CFR Part 63 Subpart JJJ -- NESHAP for
Group IV Polymers & Resins
Notes: TQ
1

## Slide 180: Federal Regulations
63 WWWW – Reinforced Plastics Composites Production
63 III – Flexible Polyurethane Foam Production
63 6O – Area Source Flexible Polyurethane Foam
63 YY – Generic MACT Acetal Resins, Polycarbonate, etc.
63 W – Group II Polymers and Resins
63 OOO – Group III Polymers and Resins
63 6L – Area Source Acrylic and Modacrylic Fiber Production
63 7H – Polyvinyl Chloride and Copolymers Production
63 6D – Area Source Polyvinyl Chloride and Copolymers
63 4H – Wet Formed Fiberglass Mat
60 HHH – NSPS for Synthetic Fiber Production
60 VVV – NSPS for Polymeric Coating for Supporting Substrates
Notes: TQ
1

## Slide 182
BACT and BARCT
Notes: TQ
6

## Slide 183: Typical Permit Conditions
Daily Emissions Limits
Gel Coat Monomer Content (weight %)
Resin Monomer Content (weight %)
Amount of Material Used
Cleaning Material
Logs

## Slide 184
Inspection Procedures

## Slide 185: Reasons for Inspections
Compliance determination
Complaint investigation
Source plan approval
Review or renewal of permits
Special studies.

## Slide 186: Pre-Inspection
Prepare inspection report form
File review
Regulation review
Equipment check
Pre-entry & entry
Pre-inspection meeting
Permit check.
Notes: TQ
18

## Slide 187: Inspection
Visible emission evaluation
General upkeep & maintenance
Maintenance records
Operational records
Any open containers?
Self-closing containers
Rags and waste in closed containers
Notes: TQ
18
TQ
19

## Slide 188
Closed Containers

## Slide 189
Open
Container

## Slide 190
Potential
Emissions??

## Slide 191
Catalyst (MEKP)
Emissions

## Slide 192
Closed Paint Containers

## Slide 193: Inspection
Coating Application Equipment
VOC content of solvents and other chemicals
MSDS
Spray Booths
Dust control equipment
  Filters and screens
  Cleaned as often as necessary

## Slide 194
Compliant
Spray Gun

## Slide 195
Spray
Booth

## Slide 196
Spray Booth Filters

## Slide 197
Filter Inspection

## Slide 198
Inspector Safety
Proper equipment
Plant evacuation
Inhalation hazards
Hazardous materials
Chemicals & Machinery

## Slide 199
Questions